Encapsulating palladium nanoparticles within a charge-assisted hydrogen bonded organic framework (CAHOF) and the catalytic performance of the heterogeneous system

Gak A.S.,1,2 Riazanov V.I.3

Student, 2th year Master

1Lomonosov Moscow State University, Faculty of Materials Science, Moscow, Russia

2A.N. Nesmeyanov Institute of Organoelement Compounds of Russian Academy of Sciences, Moscow, Russia

3Mendeleev University of Chemical Technology of Russia, Moscow, Russia

E–mail: alexandrg03@gmail.com

The size of the metal nanoparticles is inversely proportion to their catalytic performs [1]. There are several methods to promote the stabilization of metal nanoparticles to prevent self-coagulation. Herein we propose a new approach for the stabilization of small size palladium nanoparticles by encapsulating them in a charge-assisted hydrogen bonded organic framework (CAHOF) [2]. The Scheme 1 illustrate the approach. The structure of the materials was supported by elemental analysis, IR, SEM. According to SEM, data the palladium nanoparticles were distributes evenly on surface of the material samples.

Scheme 1 – The synthesis of the CAHOF stabilized palladium nanoparticles

The synthesis material proved to be a highly efficient heterogeneous catalyst of the reduction of acetylenedicarboxylic acid at a R.T., H2 balloon, in water (Scheme 2) and a Suzuki reaction at a R.T. (Scheme 3). In both cases, the chemical yield of the product was quantitative.

Scheme 2 – Reaction of reduction acetylenedicarboxylic acid

Scheme 3 – Suzuki reaction

Reference

1. Selina K. Kaiser, Zupeng Chen, Dario Faust Akl, Sharon Mitchell, Javier Pérez-Ramírez. Single-Atom Catalysts across the Periodic Table // ACS Publication, 2020.

2. Kuznetsova Svetlana A., Gak Alexander S., Nelyubina Yulia V., Larionov Vladimir A., Han Li, North Michael, Zhereb Vladimir P., Smolyakov Alexander F., Dmitrienko Artem O., Medvedev Michael G., Gerasimov Igor S., Saghyan Ashot S., Belokon Yuri N. The charge-assisted hydrogen-bonded organic framework (CAHOF) self-assembled from the conjugated acid of tetrakis(4-aminophenyl)methane and 2,6-naphthalenedisulfonate as a new class of recyclable Brønsted acid catalysts //Beilstein J. Org. Chem. (Germany), 2020, 16, 1124–1134.